## Slide 1
Base thickness and isolation dimension definitions in Speedstack
Polar Instruments Application Note AP507b
(read in conjunction with AP507)

## Slide 2
<number>
Base thickness, Tb, is the thickness of the material on the shelf in the warehouse.
Base thickness is helpful information for the PCB fabricator as a component parameter in the determination of pre-press stack thickness which, in turn, determines how many stacks can be loaded into the press.
Base Thickness
Prepreg
Tb

## Slide 3: Finished Thickness
<number>
Prepreg
Prepreg
Core
Core
100% Copper
100% Copper
The Finished Thickness, Tf, of the prepreg is its thickness after it has been pressed between two 100% solid copper sheets. Note the reduction in thickness from the base thickness, Tb. That means 100% solid; no antipads, no slots, no relief at all, all copper.
This dimension is important as we use it in the next step to determine the post–press dimensions of the board and of the impedance structures.
Tb
Tf

## Slide 4: Finished Dimensions
<number>
Prepreg
Prepreg
Core
Core
The post-press dimensions are computed from the finished thickness and from the amount of copper on each layer. The basis of the calculation is that an X% copper layer is pressed into the prepreg by an amount = (100 – X)% of the copper thickness. Thus, for example, a 20% copper (signal) layer 2 mils (2 thousandths of an inch) thick will be pressed into the prepreg (100 – 20)% of the copper thickness. That is, the copper is pressed into the prepreg by 80% of 2 mils = 1.6 mils. The 0.4 mil void will be filled by squeezed out resin. The distance between the opposing copper faces is the Isolation Distance, Tiso
Tb
Tf
20% copper pressed in 80% of its thickness
Tiso
Resin squeeze-out fills voids
90% copper pressed in 10% of its thickness
2 mils Cu
1.6 mils
Speedstack computes these post-press dimensions when finishing is applied in accordance with the thickness correction selected in the Tools/Edit Thickness option. They are then used in the impedance computation.

## Slide 5
For more information:
Contact Polar now: Phone
USA / Canada / Mexico Ken Taylor ( 503) 356 5270
Asia / Pacific
Terence Chew +65 6873 7470
Japan
Tetsuya Koizumi +81 3 3904 6230
UK / Europe Neil Chamberlain +44 23 9226 9113
Germany / Austria / Switzerland Hermann Reischer +43 7666 20041-0
www.polarinstruments.com